TENSILE PROPERTIES OF EPOXY COMPOSITES REINFORCED WITH CONTINUOUS SISAL FIBERS

W. P. Inácio(1), A. C. Pereira(1), S. N. Monteiro(2), N. T. Simonassi(1), F. M. Margem(1), R. L. Loiola(1)

arturcamposomv@hotmail.com

(1) UENF - State University of the Northern Rio de Janeiro, Advanced Materials Laboratory, LAMAV; Av. Alberto Lamego, 2000, 28013-602, Campos dos Goytacazes, Brazil (2) IME - Military Institute of Engineering.

ABSTRACT

The tensile properties of DGEBA/TETA epoxy matrix composites reinforced with different amounts of sisal fibers were evaluated. Composites reinforce with up to 30% in volume of long, continuous and aligned sisal fibers were room temperature tested in an Instron machine. The fracture was analyzed by SEM. The results showed significant changes in the mechanical properties with the amount of sisal fibers. Those properties were compared with other bend-tested composites results. The fracture analysis revealed a weak fiber/matrix interface, which could be responsible for the performance of some properties.

Keywords: sisal fiber, epoxy matrix composite, tensile properties, SEM fracture analysis.

# INTRODUCTION

In recent years climate changes and questions related to the use of non-renewable forms of energy, are favoring the use of natural materials over synthetic ones, which have a higher energy consumption associated with their processing and  fabrication procedures. A significant example is the possibility of replacement of glass fiber by natural fibers in typical composites applications(1-4). The advantage of natural fibers, especially those extracted from plants, over the glass fiber are presently a great motivation for the increasing use of “green” composites in automobiles(5-7). Glass fiber is more expensive, heavier and abrasive to processing equipment. Moreover, this synthetic fiber presents a health risk when inhaled and its production is associated with CO2 emissions. None of these shortcomings apply to lignocellulosic fibers that, in addition, are renewable, biodegradable and neutral with respect to greenhouse gases, the major responsible for global warming. According to Zah et al (7), the application of natural fiber composites is rapidly increasing in the automobile industry with annual growth rates above 20%. Both interior and exterior components are already on the market and a major reason is the technical advantage of a higher impact resistance.

Among the lignocellulosic fibers commercially available, the sisal fiber has a great potential to be selected as one of the most convenient for polymer composite reinforcement. The sisal is a bush-like plant, similar to the pineapple, native of the Amazon region in Brazil. Fibers extracted from the sisal leaves are among the strongest lignocellulosic known(8) and have been used as composite reinforcement for some time. Characterization of these composites are being carried out for different polymer matrices and mechanical tests(9-19). However, no tensile characterization was done so far for polymer composites reinforced with sisal fibers.. Therefore, the objective of this work was to conduct the tensile tests of epoxy matrix composites reinforced with sisal fibers.

# EXPERIMENTAL PROCEDURE

The sisal fiber was supplied by the firm Sisalsul, which commercializes natural lignocellulosic fibers from Brazil. The typical aspect of a sisal plantation and a lot of processed fibers are shown in Fig. 1.

Figure 1. A typical plantation of sisal in Brazil (a), a bail of processed fibers from the leaves (b) and bundle of sisal fibers used in this investigation (c).

From the as-received lot, Fig. 1(c), one hundred fibers were separated for statistic analysis of the length and diameter as shown in Fig. 2. This figure reveals a big dimensions dispersion of the sisal fibers just like other lignocellulosic fiber(1-4). Another relevant information from the histograms in Fig. 2 is that the average length of 846 mm is more than 15 times its critical length of 3 mm, obtained in epoxy pullout tests (18). This is considered a condition for long and continuous fiber(20) and assures the most effective strengthening of the matrix. It is important to mention that the statistical distribution in Fig. 2 is comparable to others recently reported on sisal fibers (18-19).

For composite fabrication, the as-received sisal fibers were initially cleaned and then dried at 60oC for 24 hours. Tensile specimens were individually prepared by laying down continuous and aligned fibers in a rectangular “dog-bone” shaped silicone mold with 5.8 x 4.5 mm of reduced gage dimensions. Fibers in amounts of up to 30% in volume were aligned along the 35 mm length of the specimens, corresponding to its tensile axis. Still fluid DGEBA/TETA epoxy resin with phr 13 was poured onto the fibers in the mold and allowed to cure for 24 hours. Seven composite specimens were fabricated for each fiber composition. Each specimen was room temperature tested in a model 5582 Instron universal machine at a strain rate of 3 x 10-3 s-1. The fracture surface of selected specimens was gold sputtered and then analyzed by scanning electron microscopy (SEM) in a model SSX-550 Shimadzu microscope operating at an accelerating voltage of 7- 15 kV.

Figure 2. Histograms for the statistical distribution of (a) length and (b) diameter of the supplied sisal fibers.

# RESULTS AND DISCUSSION

Figure 3 exemplifies the typical load vs. extension curves for different composites. These curves were recorded directly from the Instron machine and revealed that the sisal fiber reinforced composites apparently present limited plastic deformation. Consequently, these composites, in principle, may be considered as brittle materials

Figure 3. Load vs. elongation curves for epoxy composites reinforced with (a) 0%, (b) 10% and (c) 30% of volume fraction of sisal fibers.

Figure 4 illustrates the aspect of the ruptured tensile specimens corresponding to each volume fraction of sisal fiber considered for composite reinforcement. The rupture become less uniform with increasing amount of fibers This will be discussed further with the fracture analysis.

Figure 4. Tensile ruptured specimens for each volume fraction of sisal fiber incorporated into the epoxy matrix.

From the results of the load vs. elongation curves, Fig. 3, the ultimate stress (tensile strength), elastic modulus, and total strain were calculated. Table 1 shows the average values for these tensile properties for the different amounts of sisal fiber investigated.

Table 1. Tensile properties for the sisal fiber reinforced epoxy composites.

| Amount of Sisal Fiber (vol. %) | Tensile Strength (MPa) | Elastic Modulus (GPa) |
| --- | --- | --- |
| 0 | 52.38( 6.05 | 0.84 ( 0.04 |
| 10 | 60.47 ( 8.31 | 0.90 ( 0.10 |
| 20 | 83.74 ( 9.41 | 1.09 ( 0.09 |
| 30 | 112.52 ( 10.19 | 1.12 ( 0.04 |

Figure 5 plots the results of tensile strength and elastic modulus in Table 1 as a function of the volume fraction of sisal fibers. In this figure it should be noted that both the composite tensile strength and stiffness significantly increase with the sisal fiber incorporated into the epoxy matrix. An apparent linear relation exists between the tensile strength and the volume fraction of sisal fiber. In fact, in bend tests the incorporation of sisal fibers does not sensibly improve the mechanical resistance of the composite as much as in tension(14).

Figure 5 - Tensile strength variation with the amount of sisal fiber in the composite.

The results on the flexural properties in Fig. 5, of a similar sisal fiber reinforcing epoxy composites, published elsewhere(16), showed values more than 20% lower than the corresponding ones in Fig. 5. The reason for this behavior is not yet clear but might be due to the specimen processing, which was machined from a composite plate and not individually fabricated as for the tensile test in the present work. Fibers filament separation as well as debonding of the fiber/matrix interface were reported in bend tests and, in principle, could be responsible for this result (16)..

The elastic modulus variation in Fig 6 could also be adjusted to a linear relation and demonstrates a relevance increase in it values with the increase of fibers in the matrix. This can be attributed to the same mechanical proprieties analyzed for the tensile strength.

Figure 6. Variation of the elastic modulus with the volume fraction of sisal fiber reinforcing epoxy composites.

The fracture analysis of the tensile tested specimens was performed both by macroscopic observation, Fig. 4, and SEM microscopic analysis. Figure 7 shows a typical SEM fractograph of a tensile rupture specimen for an epoxy composite reinforced with 30% of sisal fiber. In Fig. 7(a) it is possible to observe a few broken fibers well adhered to the epoxy matrix. By contrast, an empty space corresponding to a fiber that was detached from the matrix can also be seen. In Fig. 7(b), the crack associated with this empty space suggests that the fiber had initially acted as a barrier for the rupture process.

Figure 7. Composite with 30% in vol. of sisal fiber, with different magnifications: 
200x (a) and (b) 500x.

# CONCLUSIONS

- The incorporation of continuous and aligned sisal fiber significantly increases the tensile strength and stiffness of DGEBA/TETA epoxy matrix composites.

- An apparent linear increase occurs up to a volume fraction of sisal fiber of 30%. This corresponds to a better performance than similar composite that were flexural tested.

- Macroscopic and microstructural evidences indicate that the strong sisal fiber acts as effective barrier for rupture propagation throughout the brittle epoxy matrix, in spite of the weak fiber matrix interface.

# ACKNOWLEDGEMENTS

The authors thank the Brazilian agencies: CNPq, CAPES and FAPERJ.

# REFERENCES

- A.K. Mohanty, M. Misra and G. Hinrichsen, “ Biofibers, biodegradable polymers and biocomposites: an overview”, Macromolecular Mat. And Engineering, 276/277 (2000), 1-24.

- P. Wambua, I. Ivens and I.Verpoest, “Natural fibers: can they replace glass and fibre reinforced plastics?”, Composites Science and Technology, 63 (2003) 1259-1264.

- Crocker, J., “Natural materials innovative natural composites”. Materials Technology, 2-3 (2008) 174-178.

- S.N. Monteiro, F.P.D. Lopes, A.S. Ferreira and D.C.O. Nascimento, “Natural fiber polymer matrix composites: cheaper, tougher and environmentally friendly”. JOM, 61(1) (2009) 17-22.

- G. Marsh, “Next step for automotive materials”. Mater. Today, 6(4) (2003) 36-43.

- S. Hill, “Cars that grow on trees”. New Scientists, 153(2067) (1997) 36-39.

- R. Zah, R. Hischier, A.L. Leão and I. Brown, “Sisal fibers in automobile industry – A sustainability assessment”. J. Cleaner Production, 15, (2007) 1032-1040.

- A.L. Leão, I.H. Tan and J.C. Caraschi, “Sisal Fiber – A Tropical natural fibre from Amazon – Potential and applications in composites”, Proceedings of the International Conference on Advanced Composites, (Hurghada, Egypt, May, 1998) 557-564.

- S.N. Monteiro, J.F. de Deus and J.R.M. d’Almeida, “Interfacial Strength of Sisal Fiber Reinforced Polyester Composites”, Proceedings of SAM-CONAMET (Mar del Plata, Argentina, 2005) 1-6.

- S.N. Monteiro, R.C.M.P. Aquino, F.P.D. Lopes, E.A. Carvalho and J.R.M. d’Almeida, “Mechanical behavior and structural characteristics of polymeric composites reinforced with continuous and aligned curaua fibers”. Rev. Mater, 11(3) (2006) 197-203.

- S.N. Monteiro, J.F. de Deus and J.R.M. d’Almeida, “Mechanical and structural characterization of curaua fibers”, Proceedings of Characterization of Minerals, Metals & Materials - TMS Conference, (San Antonio, USA, March, 2006) 1-8.

- K.G. Satyanarayana, J.L. Guimarães, F. Wypych, “Studies on lignocellulosic fibers of Brazil. Part I: Source, production, morphology, properties and applications”. Composites: Part A, 38, (2007) 1694-1709.

- S.N. Monteiro, R.C.M.P. Aquino, and F.P.D. Lopes, “Performance of sisal fibers in pullout tests”. J. Mater. Sci. 43 (2008) 489-493.

- S.N. Monteiro, A.S. Ferreira and F.P.D. Lopes, “Rupture mechanisms in composites reinforced with sisal fibers”, Proceedings of Characterization of Minerals, Metals & Materials - TMS Conference, (New Orleans, USA, March, 2008) 1-8.

- R.V. Silva, E.M.F. Aquino, L.P.S. Rodrigues and A.R.F. Barros, “Curaua/Glass Hybrid Composite: The Effect of Water Aging on the Mechanical Properties”, J. Reinforced Plast. & Comp., 28 (2009) 1857-1868.

- S.N. Monteiro, A.S. Ferreira and F.P.D. Lopes, “A comparative study of sisal fiber reinforced epoxy matrix composites as building materials”, Proceedings of the Global Symposium on Recycling, Waste Treatment and Clean Technology – REWAS2008, (Cancun, Mexico, October 2008) 1653-1658.

- R.V. Silva and E.M.F. Aquino,”Curaua fiber: A new alternative to polymeric composites”, J. Reinforced Plast. & Comp., 27(1) (2008) 103-112.

- S.N. Monteiro, A.S. Ferreira and F.P.D. Lopes, “Pullout tests of curaua fibers in epoxy matrix for evaluation of interfacial strength”, Proceedings of Characterization of Minerals, Metals & Materials - TMS Conference, (San Francisco, USA, March, 2009) 1-7.

- S.N. Monteiro, A.S. Ferreira and F.P.D. Lopes, “Izod impact energy of polyester matrix composites reinforced with aligned curaua fibers”, Proceedings of Characterization of Minerals, Metals & Materials - TMS Conference, (San Francisco, USA, March, 2009) 1-8.

- W.D. Callister Jr., Materials Science and Engineering – An Introduction, 5 ed., (New York, NY: John Wiley & Sons, 2000).

- S.N. Monteiro, K.G. Satyanarayana and F.P.D. Lopes, “High strength natural fibers for improved polymer matrix composites”, Proceedings of the International Conference on Processing & Manufacturing of Advanced Materials – THERMEC 2009, (Berlin, Germany, August, 2009) 1-6.

# Text boxes

(c)

(b)

(a)

Elongation (mm)

Load (N)

(b)

(c)

(a)

30%

20%

10%

0%