Glass Fiber and Polyester Matrix in Contact with Oil, Water and Heat: Analysis on Mechanical Properties and Final Fracture

Ricardo Alex Dantas da Cunha¹, Jayna Kátia Dionísio dos Santos1,2, Raimundo Nonato Barbosa Felipe1, Gilson Gomes de Medeiros1, Renata Carla Tavares dos Santos Felipe1

1 Federal Institute of Education, Science and Technology of RN, 59015-000– Natal, RN, Brazil.

2Graduate Program in Mechanical Engineering, of UFRN, 59072-970 – Natal, Brazil.

Abstract: Composite materials are among the new types of materials that are developed with the intention of improving the industrial prospects. These materials are aggregated to many sectors of high technology industries (aerospace, oil, marine, among others). Lately, studies have been conducted aiming the use of synthetic fiber reinforced polymer composite in the oil industry, but it is still necessary to do further analysis aiming to use these materials when in contact with oil and heat. Thus, this work purposes to study the mechanical behavior and fracture characteristics of composite produced with polyester matrix and E-fiberglass reinforcement through the hand lay-up  process. Specimens were immersed in oil and distilled water for a period of 30 days and then exposed to a temperature of 60 °C for 96 hours. After conditioning, the specimens were tested on three-point bending and characterized in relation to its final fracture. The results were compared with those obtained with specimens in the dry state, noting that, for the specimens conditioned by contact with oil and heat, there was only one change in flexural modulus, remaining virtually unchanged strength and strain flexural for all test conditions, considering, of course, their standard deviations.

Keywords: Polymer composite, fluids, heat, mechanical properties.

1. INTRODUCTION

Composite materials are also known as materials of the future, due the particularity of being formed by combining, at macroscopic level, of two or more materials that work together, functioning as a unit , to obtain a set of properties that none of the individual components present1. The composites are formed from the presence of a material known as reinforcement, which aims to interfere in the mechanical properties of the composite and matrix, acting in the implementation of mechanical stress to the reinforcement. The use of these new materials is rising due to its good mechanical properties, resistance to aggressive chemicals and effects of environmental exposure, such as radiation, humidity and temperature2.Thus, these materials can be used in environments with high temperatures 3, in addition to their high versatility in design, contributing even with minimal maintenance over time of service and an unlimited life 4.

Among the various types of reinforcement, we highlight the fibrous reinforcements, which may be synthetic and natural. Among the natural reinforcements, we can cite the fibers of pineapple, ramie, sisal and coconut, which have good mechanical and thermal properties 5. The synthetic reinforcements such as aramid fibers, carbon and glass, have a higher cost compared with natural fibers. However, glass fibers, in turn, when compared with other synthetic reinforcements, have advantages such as high mechanical strength, good commercial availability and low cost 6. With this, they are commonly used in thermoplastic composites, together with polyester resin, to produce fiberglass reinforced plastic (FRP). This composite is distinguished by having excellent mechanical properties compared to conventional metallic materials and can operate in temperature ranges of 85 to 115 °C and pressure up to 15 bar 7.

Due to the numerous advantages, fiber reinforced plastics are being used extensively as advanced materials of engineering in cutting edge technologies in the aerospace, automotive, construction and oil industries8 In the aerospace industry, these materials are present in the composition of 25% of the total weight of the fuselage sections of aircraft being used extensively in wings, tail surfaces and doors 9.In the oil sector, the polymer composites find a job in the ducts, pipes of transfer lines, floor gratings, ladders and structural steel 10.

With regard to the influence of temperature, it is known that the polymer composites withstand temperatures between 70 °C to 200 ºC. Moreover, during the curing process, in the case of thermofixed resins, there is an increase in temperature due to chemical reactions necessary for hardening. Therefore, may occur in this period the formation of microcracks and voids, and these come to influence the performance of the composite. Allied to this, when the composite is subjected to a relatively high temperature, its degradation occurs by the process of chemical decomposition of the polymer. According to the literature, the polymer, when subjected to ultraviolet radiation, is to present a low resistance, and in fact have variation in color and becomes a brittle material. Given this behavior, it is expected that the composite formed by the polymer matrix will suffer the same mechanism 11.

Thus, our objective is to determine and compare the mechanical properties of three-point bending of the composite formed by polyester resin and E-fiberglass, when immersed in various liquids such as oil and distilled water, and exposed to heat. To this end, test specimens were prepared according to ASTM D790-03. These test specimens were immersed in oil or in water for a period of 30 days and then subjected to a temperature of 60 °C for 96 hours. They were then tested for three-point bending and the results were compared with those obtained with the same material, but without being subjected to any conditioning. After these tests, the final fracture was characterized for each sample.

The period of 30 days of immersion was used because, in previous work undertaken by the authors12, it was found that immersion of the composite polyester /E-fiberglass in oil and distilled water by greater period didn’t change the mechanical properties significatively. For the preparation of this material, we used the hand lay up process, which presents a simple procedure and involves no investment in manufacturing process equipment 13.

2. MATERIALS AND METHODS

2.1 - Materials

The composite was confectioned using, as matrix, pre-accelerated orthophthalic unsaturated polyester resin, produced by the company NOVOCOL, with the following features (supplied by manufacturer): density between 1.10 and 1.15 g/cm3, viscosity BROOKFIELD, at 25 °C, between 260 and 300 cP. The catalyst used for the resin curing (time to get the complete polymerization of the compound) was methyl ethyl ketone (MEKP), manufactured by AKZO NOBEL. The material used as reinforcement was a blanket of chopped strands of E-glass, made by OWENS CORNING, with a weight of 450 g/m2. The oil used for immersion of the specimens was supplied by PETROBRAS / UN-RNCE, having an API 30.1518 (as provided by the laboratory of UN-RNCE/ATP-MO unit).

The equipments used in this study were: Pavitest universal testing machine (CONTENCO); analytical electronic scale, model FA2104N (BIOPRECISA); a muffle furnace, model F 100 (EDGCON 3P) and an optical microscope, model Pantec XJL03.

2.2 - Methods

The composite was fabricated by hand lay-up process, and the polyester resin catalyzed with 1% of catalyst in relation to the total volume of the resin, using as a reinforcement four layers of blanket of chopped strands of E-glass, obtaining, thus, a plate. After curing, specimens were cut for characterization of the composite and determination of the three-point bending properties.

3. CHARACTERIZATION OF THE MATERIAL

To characterize the material, tests were conducted, as discussed below.

3.1 - Test of Volumetric Density

The density of the composite was determined according to the procedure specified by ASTM D 792-0814. The density was calculated by averaging the results obtained with five specimens (CP), all prepared with dimensions of 25 x 25 mm.

3.2 - Test of Calcination

For this test, we used five specimens of 25 x 25 mm, which were pyrolyzed in an muffle furnace at a temperature of 450 °C for 45 min. Then we determine the volumetric fractions of reinforcement, resin and void.

3.3 - Test of Moisture Absorption

For this test, five specimens were made according to ASTM D570-0615, with the following dimensions: 25 mm in width and 76 mm in length. First, the specimens were weighted and then immersed in distilled water to reach saturation of moisture, i.e., until no significant change in mass occur. At the end of the test, we determined the total percentage of moisture absorption.

3.4 Test of Three-Point Bending

Specimens prepared in accordance with ASTM D 790-0816, with 76.09 mm x 16.04 mm x 2.9 mm (length, width and thickness, respectively), were immersed in oil or distilled water for 30 days and then heated for 96 hours at a temperature around 60 °C. For the three-point bending test, both dry specimens (not subject to immersion and heating) and specimens immersed in both fluids (oil or water) and then heated were tested. This test was performed with the Pavitest universal machine at a speed of 1 mm/min.

4. RESULTS AND DISCUSSION

4.1 - Characterization of the Composite

Determined the density of the composite and their percentages in weight of matrix, reinforcement and voids. The values are reported in Table 1.

Table 1 – Density and percentages of matrix, reinforcement and voids.

4.2 - Moisture Absorption

For composites reinforced with fiberglass, the saturation is normally reached in 2 or 3 months, with a weight increase of approximately 1.5% 17,18.However, it was observed that, for the confectioned material, the humidity saturation occurred at two and a half months, and this humidity percentage was somewhat higher. This is probably due to the fact that water has flowed by the voids of the material and also by capillary action and thus become trapped in the composite. The results are shown in Table 2.

Table 2 - Percentage of moisture absorption (%).

4.3 - Three-point Bending

As can be seen in Figure 1, the values of flexural strength remained virtually unchanged, taking into account the values of standard deviations. The results suggest that the material, once placed in distilled water and exposed to heat, presented a mechanical performance inferior to those immersed in oil or dry. But if we take into consideration the standard deviations, there is no variation in the final resistance to bending.

Figure 1: Flexural strength of the samples conditioned, compared to the original condition (dry sample).

The Figure 2 shows the results for the flexural modulus of the samples. It is observed that there was a decrease in stiffness of the material when immersed in oil and then heated.

Figure 2: Flexural modulus of the samples conditioned, compared to the original condition (dry sample).

From Figure 2, we can also say that, in the original condition, the material showed a better mechanical performance and that, when subjected to the conditioning of immersion in distilled water and heating later, the flexural modulus remained unchanged. The fall in the value of flexural modulus for the sample tested after immersion in oil and submission to the heat was probably due to the process of plasticization of the resin when in contact with oil.

In Figure 3, one can observe that the material that was subjected to contact with oil and heat suffered the greater maximum elongation. However, considering the values of deviations, these results may indicate that the maximum elongation remained almost constant.

Figure 3: Maximum deformation of the samples conditioned, compared to the original condition (dry sample).

5. CHARACTERIZATION OF FRACTURE

5.1 - Macroscopic Analysis

The following figures show the region of final fracture for the samples of the material submitted to the three different conditions of treatment.

Dry State

It can be observed that the fracture occurred in the tractioned region of the specimen, spreading to the neutral line of the material, see figure 4.

Figure 4: Specimens after the bending (dry condition), scale in mm.

Sample Subjected to Immersion in Oil and to Heat

In figure 5, it is possible to see that the material broke exactly due to bending stress, since the fracture occurred in the tractioned region and stretched out along neutral line, same condition obtained in the previous experiment.

Figure 5: Specimens after the bending (oil and temperature condition), scale in mm.

Sample Subjected to Immersion in Distilled Water and to Heat

It is observed that the fracture occurred in the tractioned region and stepped a little to the compressed region, a condition slightly different from previous, see figure 6.

Figure 6: Specimens after the bending (distilled water condition), scale in mm.

5.2 - Microscopic Analysis

Below, we present results of microscopic analysis for all conditions tested, seeking to characterize each type of fracture for a given test condition.

Dry State

In Figure 7, it can be analyzed only the characteristic of the fracture of composite in the dry state, where cracks are observed in the matrix, some of them passing behind the reinforcing material.

Figure 7: Region of fracture of the specimen in the dry state.

Figure 8 shows a region rich in resin and fracture in the matrix. In addition, it is also possible see the distribution of the reinforcing material.

Figure 8: Region of fracture of the specimen in the dry state.

Sample Subjected to Immersion in Oil and to Heat

In Figure 9, we can also observe, in the final fracture for the sample immersed in oil, cohesive cracks in the matrix and fiber and adhesive in the fiber/matrix interface. As can be seen, there is a resin-rich region and several cracks in the matrix, some of them passing behind the layer of reinforcement and longitudinal split.

Figure 9: Region of fracture of the specimen immersed in oil and heat.

In Figure 10, we observe the cross section of the specimen and the presence of dark spots in both the matrix region as the contour of the fibers. These patches were probably caused by the presence of oil, since they were not observed in other conditions.

Figure 10: Region of fracture of the specimen immersed in oil and heat.

Sample Subjected to Immersion in Distilled Water and to Heat

Figure 11 shows the final fracture of composite immersed in distilled water and exposed to heat. One observes the adhesive crack in fiber/matrix interface and cohesive cracks in resin region and fiber, beyond voids.

Figure 11: Region of fracture of the specimen immersed in distilled water and heat.

6. CONCLUSION

In the test of moisture absorption, it was observed that the material reached its saturation in period of 60 days of immersion, reaching a percentage of absorption at around 2%. This value was slightly higher, due to migration of water by capillary and voids in the material 19.

In the test of three-point bending, the results showed that the flexural modulus decreased by 30% for the condition of immersion in oil and submission to heat when compared to materials in the initial condition (dry state) or immersed in distilled water and subjected to heat. The flexural strength and deformation practically remained unchanged for all test conditions, considering the standard deviations.

With regard to the characteristic of the final fracture, there were various types of fractures in fiber/matrix interface in both the material conditioned by immersion in oil as in the material immersed in distilled water. In addition, we also observed cohesive cracks in the matrix for both test conditions.

7. ACKNOWLEDGEMENTS

To CNPq for the PIBIT scholarships granted to students, and also to PETROBRAS/UN-RNCE, by providing the oil.

8. REFERENCES

- Mendonça, P. T. R. Materiais Compostos & Estruturas-Sanduíches. Barueri: Manoele, 2005.

- Barjasteh, E., Bosze, E. J., Tsai, Y. I. and Nutt, S.R.. Thermal aging of fiberglass/carbon-fiber hybrid composites – Elsevier Science Ltda. Composites Part A. 2009; vol 49; pp 2038–2045.

- Boccaccini, A.R., Strutt, A.J., Vecchio, K.S., Mendoza, D., Chawla, K.K., Ponton, C.B. and Pearce, D.H. Behavior of Nicalon(tm)-fiber-reinforced glass-matrix composites under thermal cycling conditions. Composites A. 1998: Appl. Sci. Manufact. 29, pp. 1343–1352.

- Thomason, J. L. and Groenewoud, W. M. The infleunce of fiber length and concentration on the properties of glass fibre reinforced polypropylene: 2. Thermal properties – Printed in Great Britain. Composite Part A Jan1996; vol 27A:  pp 555-565.

- Yan, L., Yiu-wing, M. and Lin, Y. Sisal Fibre and its composites: a review of recent developments - Composites Science and Technology, Vol. 60; pp 2037-2055. April 2000.

- Almeida, S. P. S. Avaliação das Propriedades Mecânicas de Compósitos Pultrudados de Matriz Polimérica com Reforço de Fibra de Vidro – Dissertação de Mestrado – Universidade Federal do Rio de Janeiro – 2004.

- Pessanha, M. C. R., Dias, D. P., Filgueira, M., Paranhos, R. P. R. and Farias, O. L. Ensaios de tração uniaxial com variação de temperatura em adesivo utilizado em juntas coladas de tubulações de PRFV aplicado em plataformas marítimas - Revista Matéria, v. 13, n. 1, pp. 186 – 193, 2008.

- Ray, P. K., Mula, S., Bera, T. and Ray, B. C. Effects of Thermal Shocks and Thermal Spikes on Hygrothermal Behavior of Glass–Polyester Composites – Journal of Reinforced Plastics and Composites.  Nov 2007; vol 26: pp 725 – 737.

- Meyer, D. R., Bersee, H. E. N. and Beukers, A. Temperature effect on reinforced thermoplastic composite properties for primary aircraft structure applications – 49th AIAA/ASME/ASCE/AHS/ASC Structures, Structural Dynamics, and Materials Conference <br>16t 7. April 2008; Schaumburg, IL

- Costa, L. M., Cunha, P. J. A. and Rezende, C. M. Influência de Diferentes Condições Higrotérmicas na Resistência à Tração de Compósitos de Fibra de Carbono/Epóxi Modificada - Departamento de Engenharia Aeronáutica e Mecânica. ITA/SENAI, Divisão de Materiais, IAE, CTA -  Polímeros: Ciência e Tecnologia, vol. 16, n° 3, pp. 193-201,  2006.

- Noda, J., Miyano, M. N. and Nakada, M. Temperature Dependence of Accumulation of Fiber Breakages under Tensile Loading for Unidirectional CFRP Laminates. Journal of Reinforced Plastics and Composites, v. 27, n. 10, pp. 1005 – 1019, 2008.

- Dantas, C. M., Masiero, F. R. S., Felipe, R. C. S. T., Felipe, R. N. B. and Medeiros, G. G. Compósito de Matriz Poliéster e Reforço de Fibra de Vidro, Até Onde Pode Ter Contato com Petróleo - 18º CBECIMat  -  Congresso Brasileiro de Engenharia e Ciência dos Materiais, 2008, Porto de Galinhas, PE, Brasil.

- Pardini, L. C. Compósitos Estruturais: Ciência e Tecnologia - São Paulo, SP: Edgard Blücher, 2006. 313 p.

- ASTM D 792/08: Standard Test Methods for Specific Gravity and Density of Plastics by Displacement - American Society for Testing and Materials, 2008.

- ASTM D 570/06: Standard Test Method for Water Absorption of Plastics - American Society for Testing and Materials, 2006.

- ASTM D 790/03: Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials - American Society for Testing and Materials, 2003.

- Aquino, E. M. F., Sarmento, L. P. S., Oliveira, W. and Silva, R. V. Moisture Effect on Degradation of Jute/Glass Hybrid Composites. Journal of Reinforced Plastics and Composites 2007; vol. 26; 219 - 233.

- Liao, K., Shultheisz, C. R. and Hunston, D. L. Effects of Environmental Aging on the Properties of Pultruded GFRP, Composites Part A, 30: pp.  485–493, 1999.

- Dantas, C. M., Felipe, R. C. S. T. and Felipe R. N. B. Avaliação das Propriedades de Flexão do Compósito Plástico Reforçado com Fibras de Vidro Quando em Contato com Diferentes Fluidos – 10° CBPol – Congresso Brasileiro de Polímeros, 2009, Foz do Iguaçu, PR, Brasil.

Table 1 – Density and percentages of matrix, reinforcement and voids.

| Density (g/cm3) | Matrix (%) | Reinforcement (%) | Void (%) |
| --- | --- | --- | --- |
| 1.55 ± 0.2 | 72 ± 2 | 26 ± 2 | 2 ± 0.1 |

Table 2 - Percentage of moisture absorption (%).

| Moisture Content | Time |
| --- | --- |
| 2.0% | 1680 h |

Figure 1: Flexural strength of the samples conditioned, compared to the original condition (dry sample).

.

Figure 2: Flexural modulus of the samples conditioned, compared to the original condition (dry sample).

Figure 3: Maximum deformation of the samples conditioned, compared to the original condition (dry sample).

Figure 4: Specimens after the bending (dry condition), scale in mm.

Figure 5: Specimens after the bending (oil and temperature condition), scale in mm.

.

Figure 6: Specimens after the bending (distilled water condition), scale in mm.

Figure 7: Region of fracture of the specimen in the dry state.

Figure 8: Region of fracture of the specimen in the dry state.

Figure 9: Region of fracture of the specimen immersed in oil and heat.

Figure 10: Region of fracture of the specimen immersed in oil and heat.

Figure 11: Region of fracture of the specimen immersed in distilled water and heat.