PRODUCTION OF Ti-Zr-Ni  ALLOYS BY POWDER METALLURGY FOR NICKEL METAL HYDRIDE BATTERIES

J.C.S. Casini1,a; J.H. Duvaizem1; B.V. Bottiglieri1; R.R. Oliveira1; H. Takiishi1;

ajcasini@ipen.br, juliocasini@usp.br

1 Materials Science and Technology Center, Nuclear and Energy Research Institute IPEN, University of São Paulo – USP,

Av. Prof. Lineu Prestes 2242 - CEP: 05508-000 - São Paulo – Brazil

ABSTRACT

The AB2 alloys based Ti0.9Zr0.1Ni2 and Zr0.9Ti0.1Ni2 hydrogen storage alloys were prepared by powder metallurgy, using high speed planetary ball milling with speed of 200 rpm during 120 min. The samples were sintering at 1273K during 120 minutes under high vacuum. This alloy was used as negative electrode of nickel metal hydride batteries and the effects of the microstructure and electrochemical performances were investigated. The anode was prepared using a mixture of the alloy with carbon black and polytetrafluoroethylene (PTFE) used as a binder. Electrochemical measurements were performed in a standard tri-electrode system consisting of a working electrode (negative electrode), a platinum wire counter electrode and an Hg/HgO reference electrode. The electrolyte was 6 M KOH aqueous solution. Microstructure and phase composition of samples were investigated employing scanning electron microscopy (SEM) and X-ray diffraction (XRD).

Keywords: Hydrogen storage alloys, AB2 alloys, Ni-MH batteries.

INTRODUCTION

Many hydrogen storage alloys have been used as negative electrode materials of rechargeable alkaline Ni–MH batteries(1,2). At present, it is an important task to search for a new hydrogen storage alloy with a high discharge capacity for nickel metal hydride batteries.

# Among all the alloys studied, AB2-type hydrogen storage alloys have attracted the attention of investigators for their higher electrochemical capacities than that of the prevailing AB5-type rare earth-based hydrogen storage alloys.

Substitution of Ni in Ti-based Laves phase alloys has been extensively studied in order to improve the electrochemical storage capacity because of the catalytic nature of Ni. The electrochemical studies of Zr-substituted AB2 alloys reveal that the electrochemical storage capacity increases with increasing the amount of Zr. The presence of others elements in non-stoichiometric AB2 alloys leads to the improvement of the storage properties thanks to the introduction of disorder in an unchanged C14 hexagonal structure presenting modified cell parameters(3,4).

# EXPERIMENTAL

The alloys of the nominal composition Ti0.9Zr0.1Ni2 and Zr0.9Ti0.1Ni2 were prepared by powder metallurgy. The purity of starting elemental metals was higher than 99%. In order to prepare the alloy the two following steps were adopted.

In first step a binary Ti0.9Zr0.1 (17.5%Zr + 82.5%Ti) and Zr0.9Ti0.1 (5.5%Ti + 94.5%Zr) intermediary alloys were beforehand prepared by powder metallurgy using titanium and zirconium hydrogenated-powders.

The high energy planetary ball milling was using speed of 200 rpm for 120 minutes and milled powders were then cold isostatically pressed at 200 MPa, followed by sintering at 1273K (1000°C) for 120 minutes under high vacuum (10-3 Pa) and furnace cooled. The Tab.I shows the atomic and weight composition of Ti0.9Zr0.1 and Zr0.9Ti0.1 alloys.

Tab.I Atomic and weight composition of the Ti0.9Zr0.1 and Zr0.9Ti0.1 alloys.

| Compositions |
| --- |
| Nominal | Atomic (at%) | Weight (%wt) |
| Ti0.9Zr0.1 | Ti90Zr10 | 82.5Ti-17.5Zr |
| Zr0.9Ti0.1 | Zr90Ti10 | 94.5Zr-5.5Ti |

In order to prepare the ternaries alloys (Ti0.9Zr0.1Ni2, Zr0.9Ti0.1Ni2) the the following procedure was adopted. The binaries alloys (Ti0.9Zr0.1, Zr0.9Ti0.1) were hydrogenated (1 MPa H2) and after milled with nickel powder (particle size less than 45m). The high energy planetary ball milling was utilized in the same conditions previously described. The Tab.II shows the atomic and weight composition studied in this work and the respective quantity of mass (g) utilized in 10 grams of milling.

Tab.II – Nominal composition, atomic and weight of the AB2 alloys and quantity of mass (g) utilized in 10 grams of milling.

| Composition | Mass powder (g) |
| --- | --- |
| Nominal | Atomic (%at) | Weight (%wt) | Ti0.9Zr0.1 | Zr0.9Ti0.1 | Nickel |
| Ti0.9Zr0.1Ni2 | Ti30Zr3.3Ni66.7 | 25.4Ti-5.4Zr-69.2Ni | 3.07 | - | 6.93 |
| Zr0.9Ti0.1Ni2 | Zr30Ti3.3Ni66.7 | 40.2Zr-2.4Ti-57.4Ni | - | 4.25 | 5.75 |

The negative electrode was prepared using 150 mg of the blended powder with carbon black (67%) and PTFE (33%). Three-electrode set-up cell was used in this study with a Ni(OH)2 and a mercurous oxide (Hg/HgO) as the counter electrode and the reference electrodes, respectively. The electrolyte is 6M KOH solution.

The discharge capacity, activation and cycle stability of the alloy electrodes will be determined by automatic battery charge/discharge equipment. Each electrode will be charged with current density at 100 mA/g for 5h followed by a 10 min rest and then discharged at 50 mA/g to the cut-off potential of −0.6V versus the Hg/HgO reference electrode.

Samples for the microstructure studies were prepared using conventional metallographic methods. The microstructures of the specimens were examined using a scanning electron microscope equipped with energy dispersive X-ray analysis facility. Powdered samples of the alloys (<45 μm) were examined by X-ray diffraction (XRD). Identification of the various phases was carried out by comparison with standards of the ICDD data base and using the software Crystallographica Search-Match (CSM).

# RESULTS AND DISCUSSION

Backscattered electron micrographs showing a general view of the Ti0.9Zr0.1 and Zr0.9Ti0.1 alloys are shown in Fig. 1. The chemical composition of the alloys is showed in Tab III.

# Fig. 1 - Backscattered electron micrograph of the (a) Ti0.9Zr0.1 and (b) Zr0.9Ti0.1 alloys, obtained by powder metallurgy.

Tab. III. Chemical composition determined by EDX of the Ti0.9Zr0.1 and Zr0.9Ti0.1 alloys.

| Composition analyzed of alloy (at%) |
| --- |
| Alloys | Ti | Zr |
| Ti0.9Zr0.1 | 90.50 | 9.50 |
| Zr0.9Ti0.1 | 10.10 | 89.90 |

# Backscattered electron micrographs showing a general view of the Ti0.9Zr0.1Ni2 and Zr0.9Ti0.1Ni2 alloys are shown in Fig. 2. The chemical composition determined by EDX of the alloys is showed in Tab IV.

The Ti0.9Zr0.1Ni2 and Zr0.9Ti0.1Ni2 alloys are composed of two phases: the gray phase (G) and the dark gray phase (DG). The proportions of these two phases are showed in Tab. V – VI.

The Fig.3 shows XRD pattern of the Ti0.9Zr0.1Ni2 and Zr0.9Ti0.1Ni2 alloys.

# Fig. 2 - Backscattered electron micrograph of the (c) Ti0.9Zr0.1Ni2 and (d) Zr0.9Ti0.1Ni2 alloys, obtained by powder metallurgy.

Tab. IV. Chemical composition of the Ti0.9Zr0.1Ni2 and Zr0.9Ti0.1Ni2  alloys.

| Composition analyzed of alloy (at%) |
| --- |
| Alloy | Ti | Zr | Ni |
| Ti0.9Zr0.1Ni2 | 31.26 | 3.78 | 65.05 |
| Zr0.9Ti0.1Ni2 | 3.68 | 30.66 | 65.66 |

Tab. V. Composition determined by EDX of the G phase.

| Composition analyzed composition of phase G (at%) |
| --- |
| Alloy | Ti | Zr | Ni |
| Ti0.9Zr0.1Ni2 | 30.88 | 1.36 | 67.77 |
| Zr0.9Ti0.1Ni2 | 5.06 | 26.19 | 68.75 |

Tab. VI. Composition determined by EDX of the DG phase.

| Composition analyzed composition of phase DG (at%) |
| --- |
| Alloy | Ti | Zr | Ni |
| Ti0.9Zr0.1Ni2 | 52.80 | 4.48 | 42.71 |
| Zr0.9Ti0.1Ni2 | 5.00 | 62.52 | 32.49 |

# Fig 3 – XRD Pattern of the (a) Ti0.9Zr0.1Ni2 and (b) Zr0.9Ti0.1Ni2 alloys.

# According with Yu et al(5). X-ray diffraction, scanning electron microscopy and energy-dispersive X-ray analysis tests showed that the as-cast Zr-based Laves phase alloy consisted of at least eight phases. The major cubic C15-type Laves phase coexisted with the hexagonal C14-type Laves phase, orthorhombic Zr7Ni10 phase, tetragonal Zr9Ni11 phase, tetragonal ZrNi2 and a few other phases. X-ray photoelectron spectroscopy proved that Zr and Mn were richer in the outer layer of the Zr-based Laves phase hydride electrode; Ni and Cr were deficient on the surface of the electrode. After 540 charging-discharging cycles, the discharge capacities of the Zr-based Laves phase hydride electrodes decreased by 20–30%. This was mainly caused by the formation of oxides at the surface of the electrodes.

The first ten cycles and maximum discharge capacity of the negative electrodes prepared using the crushed Ti0.9Zr0.1Ni2 and Zr0.9Ti0.1Ni2 alloys are shown in Fig.4 (a) and (b), respectively.

Fig. 4 (a) – First ten cycle number of negative electrode and (b) maximum discharge capacity of the alloys.

The best performance obtained was Ti0.9Zr0.1Ni2 alloy with maximum discharge capacity of 126 mAhg-1. The Zr0.9Ti0.1Ni2 alloy showed less maximum discharge capacity (100 mAhg-1).  This result could be attribute increase of oxidation due a Zr-based Laves found in his alloy.

# CONCLUSION

The two AB2 alloys obtained a gray phase (G) and a dark gray phase (DG), but the compositions of these phases showed different. The XRD analysis showed presence of the TiNi3 phase for Ti0.9Zr0.1Ni2 alloy and Zr-based laves phase for Zr0.9Ti0.1Ni2 alloy.

The Ti0.9Zr0.1Ni2 alloy showed the best maximum discharge capacity (126 mAhg-1).

ACKNOWLEDGEMENTS

The authors wish to thank FAPESP, CNPq and IPEN-CNEN/SP for the financial support and infrastructure made available to carry out this investigation. Thanks for Soares, E. P. for assistance at experimental work. Thanks Leal Neto, R.M. for providing a Planetary Mill PULVERISETTE 5.

REFERENCES

- FERREIRA, E.A.; CASINI, J.C.S.; GALDINO, G.S.; TAKIISHI, H.; FARIA, R.N.; Microstructure and Electrochemical Properties of a LaMgAlMnCoNi Based Alloy for Ni/MH Batteries. Materials Science Forum, v. 727-728, p. 80-84, 2012.

- YOO, J-H.; SHIM, G.; CHO, S-W.; PARK, C-N.; Effects of desorption temperature and substitution of Fe for Cr on the hydrogen storage properties of Ti0.32Cr0.43V0.25 alloy. International Journal of Hydrogen Energy. v. 32, p. 2977-2981, 2007.

- XU, Y.; CHEN, C.; WANG, X.; LEI, Y.; WANG, X.; CHEN, L.; The influence of relative content of Ti and Zr on the electrochemical behavior of Laves phase alloy. International Journal of Hydrogen Energy. v. 32, p. 1716-1720, 2007.

- KANDAVEL, M.; BHAT, V.V.; ROUGIER, A.; AYMARD, L.; NAZRI, G.; TARASCON, J.; Improvement of hydrogen storage properties of the AB2 Laves phase alloys for automotive application. International Journal of Hydrogen Energy. v. 33, p. 3754-3761, 2008.

- YU, J.Y.; LEI, Y.Q.; CHEN, C.P.; WU, J.; WANG, Q.D.; The electrochemical properties of hydrogen storage Zr-Based Laves phase alloys. Journal of Alloys and Compounds. v. 231, p. 578-581, 1995.