LOW TEMPERATURE PLASMA ASSISTED CARBURIZING OF AISI 420 MARTENSITIC STAINLESS STEEL: INFLUENCE OF TREATMENT TIME

C.J. Scheuer, F.I. Zanetti, R. Pereira, T. Amaral, R.P. Cardoso, S.F. Brunatto

Grupo de Tecnologia de Fabricação Assistida por Plasma e Metalurgia do Pó – Departamento de Engenharia Mecânica, Universidade Federal do Paraná, 81531-990, Curitiba, PR, Brazil

ABSTRACT

AISI 420 martensitic stainless steel is widely used according to their good mechanical properties and corrosion resistance. However, the superior properties necessary for different applications has led to the development of a large number of researches on this subject. Plasma assisted treatment has been recommended as an option to improve surface properties of stainless steels. Among the plasma techniques, carburizing has shown good results. In this treatment, carbon diffuses into the iron crystal lattice, leading to increase the steel hardness and wear resistance. Nevertheless, when treatment is carried out at high temperature or for too long treatment time, chromium carbides precipitation occurs, resulting in a decrease of the stainless steel corrosion resistance. Aiming to determine the effect of the treatment time on surface properties of low temperature plasma carburized AISI 420 steel, carburizing was carried out for times from 4 to 16 h at a temperature of 723 K in a 99.5% (80% H2 + 20% Ar )+ 0.5% CH4 gas mixture, at a flow rate of 1.67 × 10−6 Nm3 s−1. Samples were characterized by means of confocal laser scanning microscopy, X-ray diffractometry and microhardness measurements. Results indicate that the thickness and hardness of the carburized layers increase with the carburizing time. In addition, the hardness increase of treated surfaces has been attributed to the formation of cementite and carbon expanded martensite along the obtained compound and diffusion layers.

Key-words: Low temperature plasma carburizing, AISI 420 martensitic stainless steel.

INTRODUTION

Low temperature plasma carburizing has been increasingly accepted as a hardening process for stainless steels because it produces a good combination of tribological and corrosion properties. The hardening mechanism is based on the supersaturation of the iron crystalline lattice with carbon, which greatly hardens the material surface, signiﬁcantly expands the unit cell, produces high levels of compressive residual stresses and, ultimately, leads to the occurrence of deformation bands and rotation of the crystal lattice [1-7].

In this context, by a literature survey can be easily found several papers published over the past decades, on the application of low temperature plasma carburizing treatment on austenitic stainless steel [1-8]. However, little has been published up till now for low temperature plasma carburizing of martensitic stainless steels. In this case, some works present non-promising results [9-11], while good and promising results are presented in [12,13].

Thus, seeing that the microstructural changes introduced during plasma carburizing have a signiﬁcant impact in the material surface properties, and considering that these changes are dependent of the operation variables, the effect of treatment parameters variation have been extensively studied. The knowledge of its influence allows a better selection of it in order to achieve the desired surface properties.

In this work, the effect of treatment time on growth kinetics of the compound layer produced in the AISI 420 martensitic stainless steel by low temperature plasma carburizing was investigated.

EXPERIMENTAL PROCEDURE

Cylindrical samples of 10 mm in height and 9.5 mm in diameter were cutted from AISI 420 martensitic stainless steel commercial rod. They were oil quenched from 1323 K and the austenitizing time was 0.5 h. After heat treatment, samples were ground using SiC sandpaper ranging from 100 to 1500 grade and polished using 1 μm Al2O3 abrasive suspension. Finally, samples were cleaned with alcohol in ultrasound bath and introduced into the discharge chamber, in the as-quenched condition. The hardness of the as-quenched samples was 510 HV0.3 on average. Aiming to determine the tempering effect due to plasma treatment on sample hardness, quenched samples were tempered in conventional furnace at 723 K for 1 h for comparison purpose. The hardness of the as-tempered samples was 410 HV0.3 on average.

In order to remove the native oxide layer formed on the sample surface, the specimens were sputter-cleaned by means of glow discharge using 80% H2 + 20% Ar gas mixture, 400 Pa pressure, 573 K temperature, and 0.5 h time. Plasma carburizing was carried out using gas mixture of 99.5% (80% H2 + 20% Ar) + 0.5% CH4 in volume. The gas flow rate, pressure and treatment temperature were fixed at 1.66 × 10-6 Nm3 s−1, 400 Pa and 723 K, respectively. Ranges of processing times between 4 to 16 h, were studied in the present work.

As the samples are placed as a discharge cathode, the heating of samples was obtained by plasma species (ions and fast neutrals) bombardment. The plasma apparatus, presented in Fig. 1, consisted of a 3.6 kW square-wave pulsed DC power supply and a cylindrical vacuum chamber of 350 mm in diameter and 380 mm high of stainless steel, attached to steel plates sealed with silicone o-rings at both ends. The system was evacuated to a residual pressure of 1.33 Pa using a double stage mechanical pump. The gas mixture and flux of H2, Ar and CH4 was adjusted by three mass flow controllers, two of 8.33 × 10−6 Nm3s−1 (500 sccm – standard cubic centimeter per minute) and one of 8.33 × 10−8 Nm3s−1 (5 sccm), respectively.

| 1 – Mass flow control unit | 8 – Thermal mass flow controllers |
| --- | --- |
| 2 – Power supply | 9 – Viewing window |
| 3 – Digital pressure display | 10 – Vacuum chamber |
| 4 – Gas valves | 11 – Vacuum valve |
| 5 – Capacitive manometer | 12 – Manometers |
| 6 – Multimeters | 13 – Vacuum pump |
| 7 – Gas lines | 14 – Gas cylinders |

Figure 1: Schematic representation of the plasma apparatus employed in this study

Samples were placed in the cathode and were negatively biased at 700 V pulsed dc. The mean power transferred to the plasma, and as a result the sample temperature, was adjusted by varying the switched-on time (tON) of the pulsed voltage. The temperature was measured by means of a chromel­alumel thermocouple (K­type of 1.5 mm diameter) inserted 8 mm depth into the sample holder. The pressure in the vacuum chamber was measured by a capacitance manometer of 1.33 × 104 Pa in full-scale operation and adjusted by a manual valve.

The preparation of the treated samples for the microstructual analysis was obtained by conventional metallographic procedure. After polishing, the cross-sectioned samples were etched using Vilella’s reagent. Samples were examined using a Confocal Laser Scanning Microscope (Olympus LEXT OLS 3000). The identification of the phases present in the treated layers was carried out by X­ray diffractometry (XRD) technique, using a Shimadzu XDR 7000 X­ray diffractometer with a Cu Kα X­ray tube in the Bragg-Brentano configuration. The presented microhardness profiles correspond to a mean of five measurements which was obtained using a Shimadzu Micro Hardness Tester HMV­2T, applying a load of 10 gf for a peak-load contact of 15 s. The same equipment was employed to perform surface hardness measurements applying a load of 300 gf for a same peak-load contact.

RESULTS AND DISCUSSION

Cross-section micrography of samples treated at times of 4, 8, 12 and 16 h are presented in Fig. 2 (a, b, c, d), respectively. It is to be noted that a thin and continuous surface layer is created. It can also be observed that the layer is not etched by Vilella’s reagent on treated surface, indicating the occurrence of a single-phase layer. More, there is no evidence of sensitization in the diffusion layer, since chromium carbide precipitation was not also apparent in the micrographic examinations.

The effect of treatment time on the growth of the carburized layer can also be described by the diffusion mechanism. So, the layer thickness–time dependence is present in Fig. 3 (a). It can be noted that the obtained layers are thicker to the samples treated at greatest times. Fig. 3 (b) presents the evolution of layer thickness as a function of the square root of treatment times. A linear relationship is observed for the times here investigated. This, again, confirms the dominance of atomic diffusion in the development of the precipitation-free carburized layer. From these results, it can be considered that the growth of the carburized layer can be described by the Fick’s Second Law subjected to the fixed surface boundary condition, i.e.

(1)

where d is layer thickness,  a constant,  the treatment time,  the diffusion coefficient of carbon in the layer and  is  and thus temperature-dependent. At the specific processing temperature of 723 K, the layer growth kinetics is described by

(2)

where d is in micrometer (m) and  is in hours (h). By the Eq. (2) it is clearly visible that an increase on treatment time will result in an increased layer thickness, what is in consonance with the results present in Fig. 3 (a). Very interesting results on the layer thickness increase with treatments time and temperature, for different austenitics stainless steels grades, are presented by Sun [5]. On this study, Sun demonstrate that the kinetics of layer growth depends on processing temperature and time, as well as substrate material.

It should be noted that in Eq. (2), a zero treatment time does not result in a zero layer thickness. This effect can be attributed to the faster growth of the carburized layer to the initial stages of treatment, due to higher kinetic of this phase from process, possibly related to higher plasma reactivity. It was described by Conybear [14] that for long-term treatments the advantage of process kinetics, resultant from the increased supply of carbon and from the plasma reactions with the samples surface, will not be as significant as those found in short-term treatments.

Figure 2: Cross-section micrographs of samples treated at times of: (a) 4, (b) 8 (c) 12 and (d) 16 h. Treatment carried out at 723 K, using a gas mixture composition of 99.5% (80% H2 + 20% Ar) + 0.5% CH4 at a flow rate of 1.67 × 10−6 Nm3s−1.

Figure 3: (a) Layer thickness as a function of the treatment time and (b) layer thickness as a function of the square root of the treatment time. Treatment carried out at 723 K, using a gas mixture composition of 99.5% (80% H2 + 20% Ar) + 0.5% CH4 at a flow rate of 1.67 × 10−6 Nm3s−1.

Figure 4 presents a comparative of the X-ray diffraction patterns obtained for the different carburizing time conditions analyzed and for as-quenched samples (non­plasma treated). The as quenched sample presents three peaks all attributed to the martensite phase (’) in accordance with Pinedo [15]. After treatments some significant changes can be observed: the martensite peaks were broadened and slightly shift to lower angles, indicating lattice parameter expansion and residual stress formation. From peak shift, it can be also expected that during the treatment, the carbon diffusion into the martensite phase tends to result in the enhancement of the carbon content of the super-saturated solid solution. A similar result by introducing nitrogen in martensite phase was shown in [16-18], which leads to the so-called nitrogen expanded martensite (’N phase). Here, in analogy, the low-temperature carbon alloyed martensite phase was called carbon expanded martensite ('C phase). Otherwise, peaks occurring at 39.8º, 45.9º, 71.3 º and 86.1 are in consonance with [19-21], which correspond to cementite (Fe3C). Finally, the non-existence of chromium carbides peaks for the 4, 8 and 12 h conditions, gives support to the assumption for which the corrosion resistance of the studied martensitic stainless steel would not be depleted by the treatment performed at these times. Even though some chromium could be present in the M3C carbide, there is no evidence of depletion on the corrosion resistance of the treated AISI 420 on the cross-section micrography present on Fig. 2 (a, b, c), which was etched with Vilella’s reagent. For the plasma carburizing performed at 16 h condition, it can be verified the presence of two peaks related to chromium carbide phase at diffraction angles of 37.5 º for the Cr2C phase and another at 40.5 º corresponding to Cr7C3 phase. The occurrence of these phases in stainless steels is undesirable, since these affect the corrosion resistance of this material type.

Figure 4: XRD patterns for as-quenched (untreated) sample and for samples treated at times of 4, 8, 12 and 16 h. Treatment carried out at 723 K, using a gas mixture composition of 99.5% (80% H2 + 20% Ar) + 0.5% CH4 at a flow rate of 1.67 × 10−6 Nm3s−1.

Figure 5 shows the results of surface effective microhardness of treated samples as a function of treatment times, for measurements taken at the samples top and bottom. It can be noted that the samples surface microhardness increases with increasing of carburizing time in the range between 4 and 12 h. This increase in hardness can be attributed to the addition of carbon retained in solid solution in martensitic crystalline lattice. For the treatment condition of 16 h, the surface microhardness of steel suffered a decline. This decrease is probably associated with increased of alloy carbides precipitation, which reduce the carbon held in solid solution and, consequently, the compressive residual stress in the martensite crystal lattice. This result could explain the inefficiency of the low temperature carburizing process presented by Li and Bell [10] where there was no significant increase in surface hardness for the treatment performed at 723 K, which could be explained by the long treatment time of 20 h, possibly leading to excessive precipitation of carbides. Likewise, it is observed that the hardness of the bottom surface decreases with increasing carburizing time, in the range 8 to 16 h. This is expected as an effect of tempering of the material during the thermochemical treatment, which is more pronounced at the first 60 minutes.

Figure 5: Surface effective microhardness of plasma carburized AISI 420 martensitic stainless steel samples treated at times of 4, 8, 12 and 16 h. Treatment carried out at 723 K, using a gas mixture composition of 99.5% (80% H2 + 20% Ar) + 0.5% CH4 at a flow rate of 1.67 × 10−6 Nm3s−1.

The microhardness profiles of carburized samples treated at 4, 8, 12 and 16 h are showed in Fig. 6. It can be noted that the hardness of the samples increases with increasing carburizing time in the range between 4 to 12 h. This increase in hardness confirms the addition of carbon retained in solid solution. In other hand, for the time range between 12 to 16 h, the AISI 420 steel samples hardness decreased. This decrease is related to the increase of the precipitation of second phase particles, which reduces the compressive stresses in the crystal lattice, due to the carbon content depletion kept in solid solution, in the carburized layer, as suggested by the XRD spectra. A similar behavior was observed by Pinedo [15] on plasma nitriding of AISI 420 steel at the temperature of 793 K, at times of 12 to 16 h. It can be also noted that the curves present a shift to the right, showing an increased carbon diffusion as the processing time is increased. Finally, for 16 h condition the hardness profile is displaced to the left with respect to 12 h. This result could be also related to a higher carbides precipitation for this condition. Hardness values of 636, 873, 1177 and 810 HV0.01 were measured for 4, 8, 12 and 16 h processing times, respectively, at depth of 2.3 to 4.5 μm, inside the compound layer. The depth of hardening for treatment conditions were 30, 50, 90 and 70 m. After these depths, all samples tend to the bulk hardness, about 375 HV. Only the 16 h sample showed a lower bulk hardness (345 HV0.01), which is not surprising because the alloy carbide precipitation is not restricted to the surface.

Figure 6: Microhardness profiles of plasma carburized AISI 420 martensitic stainless steel samples treated at times of 4, 8, 12 and 16 h. Treatment carried out at 723 K, using a gas mixture composition of 99.5% (80% H2 + 20% Ar) + 0.5% CH4 at a flow rate of 1.67 × 10−6 Nm3s−1.

CONCLUSIONS

A study was carried out aiming to determine the influence of the treatment time on the kinetics of low temperature plasma carburizing of AISI 420 martensitic stainless steel, and the main conclusions of the work can be listed as follows:

- Low temperature plasma carburizing can be successfully applied to improve surface hardness of AISI 420 martensitic stainless steel samples;

- The increase of the surface hardness is due to the formation of carbon expanded martensite in carburized layers and cementite ;

- The kinetics of layer growth depends on processing time. From the results, it can be concluded that diffusion is the dominant mass transfer mechanism governing the development of the carburized layer at low temperatures. the increasing of carburizing time increases the thickness of the carburized layer and also tends to induce the precipitation of carbides in the layer,. Only when the processing time sufficiently short can a precipitation-free layer be produced;

- XRD dates confirmed the presence of chromium carbides precipitates on sample treated during 16 h at 723 K. The non-existence of chromium carbides peaks on the other availed conditions gives support to the assumption for which the corrosion resistance of the martensitic stainless steel would not be depleted.

ACKNOWLEDGEMENTS

This work was supported by CNPq, CAPES-COFECUB and Programa Interdisciplinar de Petróleo e Gás Natural da UFPR (PRH24). The authors also wish to express their thanks to the Laboratory of X-ray Optics and Instrumentation – LORXI, from the Universidade Federal do Paraná (UFPR) by the use of the X-ray diffraction equipment.

REFERENCES

[1] Y. Sun, T. Bell. Dry sliding wear resistance of low temperature plasma carburised austenitic stainless steel. Wear 253 (2002) 689–693

[2] Y. Sun. Response of cast austenitic stainless steel to low temperature plasma carburizing. Materials and Design 30 (2009) 1377–1380

[3] K. Tokaji, K. Kohyama, M. Akita. Fatigue behaviour and fracture mechanism of a 316 stainless steel hardened by carburizing. International Journal of Fatigue 26 (2004) 543–551

[4] S.C. Gallo, H. Dong. Corrosion behaviour of direct current and active screen plasma carburised AISI 316 stainless steel in boiling sulphuric acid solutions. Corrosion Engineering, Science and Technology, v. 46, p. 8-16, 2011

[5] Y. Sun. Kinetics of low temperature plasma carburizing of austenitic stainless steels. Journal of Materials Processing Technology 168 (2005) 189–194

[6] Y. Ueda, N. Kanayama, K. Ichii, T. Oishi, H. Miyake. Metallurgical characteristics of the plasma (ion)-carburized layer of austenitic stainless steel SUS316L. Surface & Coatings Technology 193 (2005) 50– 54

[7] R.M. Souza, M. Ignat, C.E. Pinedo, A.P. Tschiptschin. Structure and properties of low temperature plasma carburized austenitic stainless steels. Surface & Coatings Technology 204 (2009) 1102–1105

[8] S.C. Gallo, H. Dong. EBSD and AFM observations of the microstructural changes induced by low temperature plasma carburising on AISI 316. Applied Surface Science 258 (2011) 608– 613

[9] A. Leyland, D. B. Lewisb, P. R. Stevenson, A. Matthews. Low temperature plasma diffusion treatment of stainless steels for improved wear resistance Surf. Coat. Technol. 62 (1993) 608–617.

[10] X. Y. Li, T. Bell. A comparative study of low temperature plasma nitriding, carburising and nitrocarburising of AISI 410 martensitic stainless steel. Mater. Sci. Technol. 23 (2007) 355–361.

[11] P. Stevensom, A. Leyland, M. Parkin, A. Matthews. The effect of process parameters on the plasma carbon diffusion treatment of stainless steels at low pressure. Surf. Coat. Technol. 63 (1993) 135–143.

[12] C. J. Scheuer, R. P. Cardoso, R. Pereira, M. Mafra, S. F. Brunatto. Low temperature plasma carburizing of martensitic stainless. Mater. Sci. Eng. A 539 (2012) 369–372.

[13] C.J. Scheuer, R.P. Cardoso, F.I. Zanetti, T. Amaral, S.F. Brunatto. Low-temperature plasma carburizing of AISI 420 martensitic stainless steel: Influence of gas mixture and gas flow rate. Surf. Coat. Technol. 206 (2012) 5085–5090

[14] J.G. Conybear. The role of process variables in plasma carborizing. Heat Treating, n. 3, p 24–27, 1988.

[15] Pinedo, C. E. Estudo Morfológico e Cinético da Nitretação por Plasma Pulsado do aço Inoxidável

Martensítico AISI 420. 203 f. PhD Thesis – Instituto de Pesquisas Energéticas e Nucleares. São Paulo, 2000 (in Portuguese). (accessible online in: http://pelicano.ipen.br/PosG30/TextoCompleto/Carlos%20Eduardo%20Pinedo_D.pdf, accessed in october 14, 2011).

[16] S.K. Kim, J.S. Yoo, J.M. Priest, M.P. Fewell. Characteristics of martensitic stainless steel nitrided in a low-pressure RF plasma. Surface & Coatings Technology, v. 163–164, p. 380–385, 2003.

[17] C.X. Xi, D.X. Liu, D. Han. Improvement of corrosion and wear resistances of AISI 420 martensitic stainless steel using plasma nitriding at low temperature. Surface & Coatings Technology, v. 202, p. 2577–2583, 2008.

[18] C.X. Xi, D.X. Liu, D. Han. Improvement of mechanical properties of Martensitic stainless steel by plasma Nitriding at low temperature. Acta Metallurgica Sinica (English Letters), v. 21, p. 21–29, 2008.

[19] F.M. El-Hossary, N.Z. Negm, A.M. Abed El-Rahman, M. Hammad. Duplex treatment of 304 AISI stainless steel using rf plasma nitriding and carbonitriding. Materials Science and Engineering C, v. 29, p. 1167-1173, 2009.

[20] F.M. El-Hossary, N.Z. Negm, S.M. Khalil; A.M. Abed El-Rahman, D.N. Mcilroy. RF plasma carbonitriding of AISI 304 austenitic stainless Steel. Surface and Coatings Technology, v. 141, p. 194-201, 2001.

[21] A.M. Abed El-Rahman; F.M. El-Hossary, N.Z. Negm, N.Z. Prokert, F. Richter, W Möller. Influence of gas pressure and substrate temperature on PIII nitrocarburizing process of AISI 304 stainless steel. Nuclear Instruments and Methods in Physics Research B, v. 226, p. 499-506, 2004

# Text boxes

H2

Ar

CH4

1

2

3

8

11

5

4

6

10

14

12

13

9

7

(b)

20 m

(a)

(d)

20 m

20 m

(c)

20 m

(a)

(b)